## Slide 1
c = 28,750 Å from XRD
c = 19,217 Å from XRD
In
Se
A
B
C
Rhombohedral (3R)
Space group R3m
A
B
A
Hexagonal (2H)
Space group P63/mmc
In2Se3 α phase: Fundamental Properties of the Quintuple Layer monolayer

## Slide 2
In2Se3 α phase: ARPES : conduction band
ACS Nano 2023, 17, 19, 18924–18931 (2023)

## Slide 3
In2Se3 on WSe2 heterostructure
1
2

## Slide 4
In2Se3 on WSe2 heterostructure
1
2
A1(LO + TO)
A1(LO)

## Slide 5
In2Se3 on WSe2 heterostructure
1
2
10 µm
a)
c)
b)
d)
e)
f)
2 µm

## Slide 6
In2Se3 on WSe2 heterostructure
1
2
10 µm
a)
b)
c)

## Slide 7
In2Se3 on WSe2 heterostructure
1
2
Integration In
10 µm
a)
b)
c)

## Slide 8
In2Se3 on WSe2 heterostructure
1
2

## Slide 9
In2Se3 on WSe2 heterostructure
a)
b)
c)
d)
Δk
ΔE
ΔER = 0,235 ± 0,01 eV
ΔkR = 0,245 ± 0,01 Å-1
αR = 1,9 ± 0,2 eV Å

## Slide 10
In2Se3 on WSe2 heterostructure
1
2